## Slide 1: Data from a thick Nb3Cl8 sample for multi-slice ptychography
Zhen Chen
5/6/2018
Cornell University
School of Applied and Engineering of Physics

## Slide 2
13.375 Å
Annular dark-field image
scan position average diffraction
Phase
Structure model of this sample
ptychography
probe from ptychography
Single-slice Ptychography: Thickness limited resolution
0.67Å
Thickness of this sample is ~4 nm. The basic structure can be resolved from single-slice ptychography, but the 0.67 Å Nb-Nb dumbbell cannot be resolved.
Nb
Cl
Amplitude
dataset 83
parameters:
voltage 120 kV
convergence angle 24 mrad
rotation angle 30⁰
scan step 0.43 Å
Notes: 83

## Slide 3
ePIE from a thicker sample
semi-convergence angle α=24 mrad, electron energy 120 keV
Annular dark-field image
scan position average diffraction
Phase
Amplitude
Single slice ptychography
Thickness of this sample is ~16 nm
Thickness limit for a resolution 0.67 Å (using the equation below) is ~7nm
dataset 17
Notes: 17

## Slide 4
Phase
Amplitude
ePIE of dataset from a bilayer WS2/MoSe2 sample
parameters:
voltage 80 kV
convergence angle 21.4 mrad
rotation angle 30⁰
scan step 0.85 Å
defocus ~56 nm